# SECTION 091900

WATER REPELLENTS

This guide specification has been prepared to assist design professionals in the preparation of a specification section covering Anti-Graffiti Coatings. It may be used as the basis for developing either a project specification or an office master specification.

PART 1 - GENERAL

## 1.01       SECTION INCLUDES:

Specifier Notes: Edit the following to suit project requirements; delete substrates not receiving water repellent.

- Clear penetrating water repellent coating applied to exterior [vertical] [concrete] [masonry] [stone] [______] surfaces.

- Extended written warranty

Specifier Notes: Edit the following paragraphs to suit project requirements; list only those sections specifically applicable to the work of this section.

### 1.02      RELATED SECTIONS:

Section [033000 – Cast-In-Place Concrete] [034100 – Structural Precast Concrete] [034500 – Architectural Precast Concrete] [03470 – Tilt-Up Precast Concrete] [042000 – Unit Masonry] [044000 – Stone]

  - REFERENCES:

#### Comply with the provisions of the following standards for concrete [______] surfaces.

A.    ASTM D6578  “Standard Practice of Determination of Graffiti resistance”

1.04	SUBMITTALS:

A.	Comply with Section ________, unless otherwise indicated.  Substitution requests must be submitted 14 			days prior to bid date.

B.    Product Data: Manufacturer’s specifications and technical data including the following:

1.     Detailed specification of construction and fabrication.

2.     Manufacturer’s installation instructions.

3.     Corporate Letter of Compliance to section 1.5 D Product Performance Characteristics

C.    Quality Control Submittals:

1.     Statement of qualifications.

2.     Statement of compliance with Regulatory Requirements.

3.     Field Quality Control Submittals as specified in Part 3.

4.     Manufacturer’s field reports.

1.05	QUALITY ASSURANCE

- Manufacturer’s Qualification:

- 10 years experience in the actual production of specified product.

- Manufacturing facility has achieved ISO 9001 Quality and ISO 14001 Environmental certifications.

- Installer’s Qualifications:

- Firm experienced in installation or application of systems similar in 				complexity to those required for this Project.

2.	Acceptable to or licensed by manufacturer.

3.	Not less than 3 years experience with systems.

4.	Successfully completed not less than 5 projects using this system.

- Pre-Application Testing Project Mockup:

1.	Test graffiti resistance on a mockup.

2.      Comply with installation requirements of this Section.

3.      Inspect mockup for signs of reactions with the surface, streaks, discoloration, insufficient penetration and improper water repellency.

- Product Qualifications:

Comply with the provisions of the following standards for concrete (precast, cast-in-place).

1.     Active Content: Organosiloxane.

2.     Solvent: water

3.     ASTM D 6578 “Graffiti Resistance”

Cleanability level of 3 after 10 cycles

4.     Surface Appearance: No appreciable difference compared to non-coated surface.

Note: All testing must be performed by an independent laboratory approved by the engineer.

- Regulatory Requirements: Products must have independent laboratory analysis that material does not contain any known carcinogens.  If used indoors the material must comply with the following safety requirements:

  - Complies with State and Local regulations concerning AIM (Architectural, Industrial, and               Maintenance) coatings regarding VOC (Volatile Organic Content)

1.     Flammability, Smoke Spread and Toxic Fume Emission During Burning (BS 6853)

2.     Toxic gases below IDLH level.

3.     Flame Propagation: Does not propagate flame

4.     Smoke emission: No change

Specifier Notes: Include requirement B on projects listed in AZ, CA, OR, and WA. This requirement may also be useful on projects seeking LEED certification.

- Contains no chemicals listed on the CalProp65 harmful chemicals list.

1.06	DELIVERY STORAGE AND HANDLING

A.	Packing and Shipping: Deliver products in original unopened packaging with legible manufacturer’s 			identification.

B.	Storage and Protection:	 Comply with manufacturer’s recommendations.

1.07	PROJECT CONDITIONS

A.	Environmental Requirements:

1.	Maintain ambient temperature above 40 degrees F during and 24 hours after installation.

2.	Do not proceed with application on materials if ice or frost is covering the substrate.

3.	Do not proceed with application if temperature of surface exceeds 90 degree F.

4.	Do not proceed with the application of materials in rainy conditions or if heavy rain is anticipated 				within 4 hours after application.

B.	Sealer Coordination:

1.	Verify compatibility with curing compounds, patching materials, repair mortar, paints, sealants, etc. 				to be used on concrete surfaces to ensure compatibility with the anti-graffiti coating.

1.08	WARRANTY REQUIREMENTS

A.   The system manufacture shall furnish the Owner a written single source performance warranty that the Anti-Graffiti Coating System will be free of defects related to workmanship or material deficiency for a five (5) or ten (10) year period from the date of completion of the work provided under this section.

The following performance standards shall be specifically covered under the warranty:

1 The Anti-Graffiti coating will withstand a minimum of 10 cleaning cycles before the need to retreat the substrate.

2.    All defective areas shall be retreated by the system manufacture as determined by the Engineer.

3.		The Anti-Graffiti Coating Manufacturer shall be responsible for providing material to reseal areas of the concrete where sealer effectiveness does not meet the specified limits.

PART 2 - PRODUCTS

2.01	MANUFACTURER

A.	Acceptable manufacturers and products:

1.	Protectosil® ANTIGRAFFITI-US

Evonik Corporation: 2 Turner Pl; Piscataway NJ, 08854; 800-828-0919

2.	Others as they provide a Corporate Letter stating that they comply with all the requirements of Section 1.3 References, 1.5 D. Product Qualifications 1.5 E Regulatory Requirements and 1.8 Warranty Requirements.

PART 3 - EXECUTION

3.01 	EXAMINATION

A.	Verification of Conditions: Examine areas and conditions under which work is to be performed and

identify conditions that may be detrimental to proper or timely completion.

1. 	Do not proceed until unsatisfactory conditions have been corrected.

  - PREPARATION

- Protection: Install coverings to protect adjacent surfaces.

B.    Surface Preparation:

1.   Surfaces to receive anti-graffiti coating shall be cleaned of dirt, oil, grease, laitance, and other contaminants. Oil, grease and other automotive contaminants shall be removed with degreasers. All other surfaces shall be cleaned by mid-pressure water (1500 psi).   High pressure water is the minimum cleaning that will be accepted, other methods, such as blastracking, mobile power scrubbing and sandblasting may be submitted.

2.	Remove dirt, dust and materials that will interfere with the proper and effective application of the anti-graffiti coating. It is the responsibility of the Contractor to prepare the surfaces of the concrete as recommended by the Anti-graffiti Manufacturer and acceptable to the Engineer

3.     Check the compatibility of all caulking and patching material to be used with the anti-graffiti coating.

4.     Sealants, patching materials, and expansion joints shall have been installed and approved.

3.03	FIELD QUALITY CONTROL

A.    Alcohol Test: After anti-graffiti coating has dried, spray coated surfaces with isopropyl alcohol.

1.     After surfaces have adequately dried, recoat surfaces that show absorption of the alcohol.

B.    Manufacturer’s Field Services:

1.	Furnish written certification that surface preparation method and final condition has manufacturer’s approval and comply with the warranty.

2.	Test area: Furnish results of test area absorption on each type of substrate. Test results shall determine application rate.

C.    Test Area:

1.	Before application, the following field evaluation will be done. The cost of the field testing will be the responsibility of the Manufacturer.

2.	Prepare a three feet by three feet area to be sprayed with the anti-graffiti coating. The area will be determined by the Owner. Apply the anti-graffiti coating as per manufacturer’s instructions.

3.     Allow seven days for the sample to cure run the alcohol splash test on the treated area.

Owner or owner’s rep must be present for the application of the Antigraffiti coating and the test.

4.	Acceptable results are as stated in the warranty provisions. Coverage rate used to pass this test section must be used on entire project.

3.04     APPLICATION

- Follow manufacturer’s instructions for application and coverage, and procedures established during preparation of mockup Product shall be applied as supplied by the manufacturer without dilution or alteration.

B.	Apply at temperature and weather conditions recommended by the manufacturer or written in this specification.

C.	Follow manufacturers’ recommendations concerning protection of glass, metal and other non-porous substrates.  Contractor will be responsible to clean all surfaces that are contaminated by the water repellent.

D.    Follow manufacturer’s recommendation concerning protection of plants, grass and other vegetation.

Contractor will be responsible for replacing all plants, grass or vegetation damaged by the water repellent.

E.    Surface residue shall be brushed out thoroughly until they completely penetrate into the surface.

F.	Protect treated areas from rain and other surface water for a period of not less than four hours after application.

G.    Provide adequate ventilation and follow all safety regulations for the City, County and State.

3.05     CLEANING

A.	While Work Progresses: Clean spillage and overspray from adjacent surfaces using materials and methods as recommended by water repellent manufacturer.

B.	Remove and dispose of all materials used to protect surrounding areas following completion of the work of this section.

C.	Clean site of all unused anti-graffiti coating, residues, rinse water, wastes, and effluents in accordance with environmental regulations.

D.	Repair, restore, or replace to the satisfaction of the Architect, all materials, landscaping, and nonmasonry surfaces damaged by exposure to water repellents.

3.06     COMPLETION

A.	Work that does not conform to specified requirements shall be corrected and/or replaced as directed by the Owners Representative at contractor’s expense without extension of time.

END OF SECTION